## Slide 1
Chemical synthesis and self-assembly
of nanoparticles for plasmonics
Lise-Marie LACROIX
LPCNO – UPS, Toulouse
lmlacroi@insa-toulouse.fr
Erik DUJARDIN
CEMES - CNRS, Toulouse
dujardin@cemes.fr

## Slide 2
veimages.gsfc.nasa.gov
106 m
103 m
1 m
10-2 m
10-9 m
10-6 m
www.comté.com
Nanoparticles - introduction
Ecole ETPMSE – 20/06/2016

## Slide 3
veimages.gsfc.nasa.gov
106 m
103 m
1 m
10-2 m
10-9 m
10-6 m
www.comté.com
Nanoparticle : assembly of few thousands of atoms :
Unprecedented physical properties
Nanoparticles - introduction
Plasmonic
Magnetism
Luminescence
Ecole ETPMSE – 20/06/2016

## Slide 4
Plasmons in nanoparticles – a long history
Deruta dish :
(Cu/Ag NPs)
Medieval stained glass :
Au NPs - red color
4th century
16th century
12-14th centuries
Lycurgus cup :
(Au/Ag NPs)
1857
Michael Faraday :
Synthesis and
optical properties of NPs
1908
Collection Véga
Baccarat
Slide that Faraday used in his lecture on gold sols, in 1858.
© Whipple Museum (Wh.0654)

## Slide 5
Detection
Treatment
Nanoparticles – Present applications
Sensors
Gauges
Disque dur
Microelectronics
Ecole ETPMSE – 20/06/2016

## Slide 6
B Lamprecht et al., App. Phys. Lett., 2001, 79, 51
J. Krenn, et al., Europhys. Lett., 2002, 60, 663.
Propagation & decay.
S. I. Bozhevolnyi, A. Dereux et al.,
Opt. Exp. 2009, 34, 310
Interconnection.
l
l
l
S
J. C. Weeber et al., PRB, 2001, 64, 045411
W. L. Barnes, et al., Nature, 2003, 424, 824
Confinement.
Challenges in top-down plasmonics …
Notes: Plasmonics has emerged from the patterning of metal films, among other possible applications, in order to CONFINE, PROPAGATE and ROUTE surface plasmons beyond the diffraction linits of dielectric optics. While this was successfully demonstrated in 1-micron wide waveguides, it turned out to be very challenging to push it to real sub-wavelength devices. In particular surface roughness was creating dissipation channels which prevented long range propagation in narrow waveguide.

## Slide 7
M. Salerno, et al., Optics Commun., 2005, 248, 543.
Pushing the resolution with LSP.
Using coupled particles to confine light
In less than 100 nm wide waveguides
Optical near-field results from the superposition of
- particle plasmon near field
- interference of incident and emitted fields
Loss in 50 nm dot separated by 75nm
3dB / 15 nm
Loss in 25 nm PERFECT dots separated by 75 nm
3dB / 500 nm
M. Salerno, et al., Optics Commun., 2005, 248, 543.
H. Ditlbacher, et al., Phys. Rev. Lett., 2005, 95, 257403.
… meet assets in colloidal plasmonics
Notes: One trick was to replace continuous metal stripes by series on metal islands patterned by EBL. While this was successful to reduced the lateral dimensions of the waveguide, dissipation due to disorder and lack of cristallinity remained.
One experiment in 2005 was timely to show the assets of nanoparticles.
The performances of two Ag nanowires were compared, one done by EBL patterning of a metal film, the other one (of identical dimensions_ grown by colloidal chemistry. Injecting light in one end and monitoring the light scattered in the near-field showed that Fabry Perot cavity modes could be seen atop the crystallline nanowire but not on the rough and polycrystalline stripe.

## Slide 8
Chemical synthesis: brief overview
Perspectives : hybrids nanoparticles
Size and shape control
Nanoparticles : synthesis - applications
20 nm
Controlled self-assemblies
Ecole ETPMSE – 20/06/2016
Notes: 8

## Slide 9
X
L
L
L
“Chemical approach”
“Physical approach”
Nucleation
Growth
Self-assembly / coalescence
Liquid phase
Gas phase
General strategy for NPs synthesis
Ecole ETPMSE – 20/06/2016

## Slide 10
X
L
L
L
“Chemical approach”
“Physical approach”
Relatively low cost
Ultra high vacuum set up.
Ecole ETPMSE – 20/06/2016
General strategy for NPs synthesis

## Slide 11
X
L
L
L
“Chemical approach”
“Physical approach”
60 nm
Liquid phase reaction :
colloidal solution
Ultra high vacuum reaction :
NP onto a substrate
Ecole ETPMSE – 20/06/2016
General strategy for NPs synthesis
Surfactants
+

## Slide 12
X
L
L
L
“Chemical approach”
Ecole ETPMSE – 20/06/2016
General strategy for NPs synthesis - surfactants
Surfactants
+
Steric hindrance: polymer
Electrostatic hindrance: charges
Electrosteric hindrance:
surfactants

## Slide 13
Noble and plasmonic metal (Au, Ag, Pt, Pd) : stable in air
For noble metal : various precursors can be used!.
X
L
L
L
Ecole ETPMSE – 20/06/2016
Easy to handle! (cf TP3)
General strategy for NPs synthesis - precursor
HAuCl4, AuCl(PPh3), AuCl, AuBr….

## Slide 14
+ surfactants
Reducing agent, T
seeds + atoms
Decomposition
Nucleation
Growth
and/or Coalescence
Colloidal solution
Ecole ETPMSE – 20/06/2016
General strategy for NPs synthesis - precursor
X
L
L
L
“Chemical approach”

## Slide 15
E0 (V)
Au+ Au
Pt2+ Pt
Ag+ Ag
Cu2+ Cu
Ni2+ Ni
Co2+ Co
Fe2+ Fe
Noble metal : easy to reduce
Strong reducing agent needed
Issues of oxidation in air
1,69V
0,34V
-0,44V
Too difficult to reduce
Ecole ETPMSE – 20/06/2016
Oxydo-reduction potential :
General strategy for NPs synthesis – reducing agent
NaBH4, citrate, oleylamine, H2,….
Very easy to reduce : a variety of reducing agent can be used

## Slide 16
Synthesis : Reduction of a metallic salt
Mn+ + n e- M
Au
Ag
Ecole ETPMSE – 20/06/2016
Synthesis of nanoparticles – Brust reaction
HAuCl4
Sodium citrate
+
NaBH4
DI water, Tamb
Fast reduction

## Slide 17
Chemical synthesis: brief overview
Perspectives : hybrids nanoparticles
Size and shape control
Nanoparticles : synthesis - applications
20 nm
Controlled self-assemblies
Ecole ETPMSE – 20/06/2016
Notes: 17

## Slide 18
Size and shape control
x
y
z
E
(radius a)
E. D. Palik, Handbook of Optical Constants of Solids, Academic,
San Diego, CA 1998.
A single metal particle is modeled by a polarizable sphere
which acquires a dipolar momentum.

## Slide 19
Size and shape control
x
y
z
E
Main axis a
Minor axis b
For an elongated nanoparticle, the polarizability is no more scalar but a tensor.
E. Dujardin, C. Girard, Handbook of Nanophysics, 2010, Chp 27
C. R. C. Wang et al., J. Phys. Chem. B, 1997, 101, 6661-4

## Slide 20
Effect of nanorod aspect ratio
Wang S, Xi W, Cai F, Zhao X, Xu Z, Qian J, He S. Theranostics 2015; 5(3):251-266

## Slide 21
Effect of nanorod aspect ratio
S. Wang, W. Xi, F. Cai, X. Zhao, Z. Xu, J. Qian, S. He, Theranostics 2015; 5(3):251-266
Technological relevance of controlling the aspect ratio

## Slide 22
Es-Souni M and Habouti S, Front. Mater. 2014, 1,19
Molding of nanorods in porous alumina
P Evans, W R Hendren, R Atkinson, G A Wurtz,
W Dickson, A V Zayats and R J Pollard
Nanotechnology, 2006, 17, 5746

## Slide 23
Xia Y et al., Angew. Chem. Int. Ed., 2009, 48, 60-103.
Growth inhibition yields crystalline and faceted nanoparticles

## Slide 24
Seeds: 3-4 nm
Inhibitor: C16-NMe3+, Br- (CTAB)
Reducing agent: Ascorbic acid
Typical length: 400 nm
C. Johnson, et al., J. Mater. Chem., 2002, 12, 1765
Nanorods
<112> + <100>
A (1-11)
B (311)
C (220)
a (-200)
b (020)
C (220)
Nanorods and nanowires
CTAB
J. Gao, C. M. Bender, C. J. Murphy, Langmuir 2003, 19, 9065–9070
Cetyl trimethyl ammonium bromide
Br-
Br-
Zipping mechanism

## Slide 25
A (220)
a 1/3 (422)
b (422)
A
a
b
Seeds: no no
Inhibitor: PVP PVP/NO3-
Reducing agent: PVP PVP
Typical size: 150nm 500nm
Nanoprisms
J. Sharma, E. Dujardin, 2016, in prep.
Nanoprisms and microplatelets
PVP
Poly-vinyl pyrrolidone
J. Sharma, E. Dujardin, 2016, in prep.
Zipping mechanism
S. Bolisetty et al.,
J. Coll. Interf. Sci. 361 (2011) 90
20 mm

## Slide 26
An infinite playground
Marek Grzelcza et al.,
Chem. Soc. Rev., 2008,37, 1783
M. Rycenga et al., Chem. Rev. 2011, 111, 3669–3712

## Slide 27
An infinite playground
Marek Grzelcza et al.,
Chem. Soc. Rev., 2008,37, 1783
G. C. Schatz,
Proc. Natl. Acad. Sci. U. S. A. 2007, 104, 688

## Slide 28
Scale bars: 200 nm
TPL experiments
S. Viarbitskaya, et al.,
Nature Materials, 2013, 12, 426-432
Appl. Phys. Lett. 2013, 103, 131112
Spatial engineering of plasmonic LDOS

## Slide 29
Chemical synthesis: brief overview
Perspectives : hybrids nanoparticles
Size and shape control
Nanoparticles : synthesis - applications
20 nm
Controlled self-assemblies
Ecole ETPMSE – 20/06/2016
Notes: 29

## Slide 30
Coupled nanoparticles
y
z
x
E0
Two coupled spherical particles
R
(a)
(b)
By combining E(ra,w) and E(rb,w) into
one vector e(w) (same for E0), one gets :
With
and
All one needs is
C. Girard, Rep. Prog. Phys., 68, 1883 (2005)

## Slide 31
Coupled nanoparticles
w0
w0(1+a0/2R3)
w0(1-a0/R3)
Transverse and longitudinal modes
E0
y
z
x
R
(a)
(b)
With the simple analytical model:
Transverse
Longitudinal
N=1
N=8
C. Girard, Rep. Prog. Phys., 68, 1883 (2005)

## Slide 32
Assembling nanoparticles
C. Polte, CrystEngComm, 2015, 17, 6809-6830

## Slide 33
Adv Mater 2005, 17, 2553-59
Adv. Funct. Mater. 2011, 21, 851–859
Phys Rev Lett 2006, 97, 100801
Phys Rev B 2010, 81, 153412
J. Chem. Phys., 2009 130, 03470
ACS Nano 2012, 6, 3434-40
Plasmonic Nanoparticle Networks
Citrate-stabilized
Au NP
Mercaptoethanol (MEA)
HS-CH2-CH2-OH

## Slide 34
Nanoparticle chains
S. J. Barrow et a;., Nano Lett. 2011, 11, 4180
250 nm
65 nm
~1 nm

## Slide 35
Adv Mater 2005, 17, 2553-59
Adv. Funct. Mater. 2011, 21, 851–859
Phys Rev Lett 2006, 97, 100801
Phys Rev B 2010, 81, 153412
J. Chem. Phys., 2009 130, 03470
ACS Nano 2012, 6, 3434-40
Plasmonic Nanoparticle Networks

## Slide 36
EELS imaging & spectroscopy
2.45 eV
1.61 eV
Multimodal plasmonics in fused colloidal networks
A. Teulle, M. Bosman, C. Girard, K. L. Gurunatha, M. Li, S. Mann, E. Dujardin,
Nature Materials, 2015, 14, 87
1.11 eV
Delocalized modes in fused PNN
0.38 eV

## Slide 37
Nanorod chains
DMF:H2O 20%
DMF:H2O 6%
Z. Nie et al., Nat Mater. 2007, 6, 609

## Slide 38
Fused nanorod chains
González-Rubio, G et al., Nano Lett. 2015, 15, 8282

## Slide 39
Capillary force assisted assembly
T. Jägeler-Hoheisel, et al.
J. Phys. Chem. C, 2013, 117, 23126−23132
Long-range coupling of LSP modes
Templated 2D assembly

## Slide 40
Polarization dependency
Modal & spatial extension of coupled LSP
h = 150 nm
h = 120 nm
h = 101 nm
diameter = 100 nm
T. Jägeler-Hoheisel, et al.
J. Phys. Chem. C, 2013, 117, 23126−23132
Templated 2D assembly

## Slide 41
Chemical synthesis: brief overview
Perspectives : hybrids nanoparticles
Size and shape control
Nanoparticles : synthesis - applications
20 nm
Controlled self-assemblies
Ecole ETPMSE – 20/06/2016
Notes: 41

## Slide 42
Ecole ETPMSE – 20/06/2016
Synthesis of hybrids NPs
Alloy
Dumbbell
Core-Shell
Can we combine several properties within the same object?

## Slide 43
Ecole ETPMSE – 20/06/2016
Synthesis of hybrids NPs
Dumbbell
H. Yu et al., Nanolett. 5, 379 (2005)
Successive synthesis in organic phase

## Slide 44
Ecole ETPMSE – 20/06/2016
Synthesis of hybrids NPs : Au+Fe3O4
C. Xu et al., J. Am. Chem. Soc. 131, 4216 (2009)
Au 8nm, Fe3O4 14nm
Application : Target-specific cis-platin delivery
Herceptin
(cell targeting)
Cis-platin
(treatment)
Combination of 2 types of surface chemistry….

## Slide 45
Ecole ETPMSE – 20/06/2016
Synthesis of hybrids NPs : Au+Fe3O4
H. Yu et al., Nanolett. 5, 379 (2005)
Au 3nm, Fe3O4 14nm
Au 8nm, Fe3O4 14nm
Combination of plasmonic and magnetic properties….
Can we improve the properties?

## Slide 46
Synthesis of hybrids NPs : M@Au
Ecole ETPMSE – 20/06/2016
+Au
Hetero-epitaxy growth of Au islands
F. Wetz et al., Angew. Chem. Int. Ed 46, 7079 (2007)

## Slide 47
Synthesis of hybrids NPs : M@Au
Ecole ETPMSE – 20/06/2016
+Au
F. Wetz et al., Angew. Chem. Int. Ed 46, 7079 (2007)
Hetero-epitaxy growth of Au islands

## Slide 48
Synthesis of hybrids NPs : Co@Au
Ecole ETPMSE – 20/06/2016
Addition of a wetting layer : Sn
S. Lentijo et al., ACS Nano, 9, 2792 (2015)

## Slide 49
S. Lentijo et al., ACS Nano, 9, 2792 (2015)
Ecole ETPMSE – 20/06/2016
Synthesis of hybrids NRs : Co@Au
Good magnetic and plasmonic properties
Chemical stability

## Slide 50
Ecole ETPMSE – 20/06/2016
Synthesis of hybrids NRs : Co@Au
Aim : new biodetection based on magnetic/plasmonic NRs
A. Schrittwieser et al. ACS Nano, 6, 791 (2012)
A. Schrittwieser et al. ACS Appl. Matter Interf., 8, 8893 (2016)

## Slide 51
Ecole ETPMSE – 20/06/2016
Synthesis of ultrathin Au NWs : electronic transport
HAuCl4 + 40 Oleylamine + 100 TIPS
Hexane, 40°C
2µm
Oleylamine
Triisopropylsilane
H. Feng et al. Chem Comm. 15, 1984 (2009)
A. Loubat et al. Langmuir, 30, 4005 (2014)
d = 1.7 nm; l = 3 µm
Quantification phenomena ?

## Slide 52
Nanoxerography technique
    a) Charge injection by AFM in PMMA electret
    b) Immersion in the colloidal solution
    c) Washing : NPs trapped on the charged patterns
Motif -5V
Au NWs :
Negatively charged
in hexane!
First assembly of anisotropic NPs!
P. Moutet et al. Langmuir, 31, 4106 (2015)
Ecole ETPMSE – 20/06/2016
Single Au NWs connection

## Slide 53
Ecole ETPMSE – 20/06/2016
Single Au NWs connection
0V
1.5V
0 nm
5 nm
KFM
AFM
Fine tuning of the charge injection
P. Moutet et al. Langmuir, 31, 4106 (2015)

## Slide 54
Ecole ETPMSE – 20/06/2016
Au NWs instability
L.-M. Lacroix et al. J. Am. Chem. Soc. 136, 13075 (2014)
Raul Arenal - INA

## Slide 55
b)
a)
b)
L.-M. Lacroix et al. J. Am. Chem. Soc. 136, 13075 (2014)
Ecole ETPMSE – 20/06/2016
Au NWs instability : single chain formation

## Slide 56
Au
Pt
Pt
Ge
CoPt
Au
Co@Fe
Co@Cu

## Slide 57
Heat : thermodecomposition
thermolysis
Mechanic vibration : sonolysis
Irradiation : UV decomposition
Ecole ETPMSE – 20/06/2016
Synthesis of nanoparticles – Energy transfer

## Slide 58
Ecole ETPMSE – 20/06/2016
Synthesis of hybrids NPs
Dumbbell
H. W. Gu Yu et al., J. Am. Chem. Soc. 127, 34 (2005)
Synthesis in aqueous and organic phase

## Slide 59
15 min
L ~ 100 nm
45 min
L ~ 500 nm
3 h
L  2 µm
Growth mechanism : isotropic environment
A. Loubat et al. Langmuir, 30, 4005 (2014)
10 mM HAuCl4+ 400 mM OY + 1000 mM TIPS
Au NWs
Hexane
,
40°C, 1h30
Notes: Signal plus simple
Plus gde gamme en vecteur de diffusion car SWING : plus d’info notamment les NWs

## Slide 60
Growth mechanism : isotropic environment
Au NWs : yield 75%
Oriented attachment
Atom/atom growth
15 min
L ~ 100 nm
45 min
L ~ 500 nm
3 h
L  2 µm
Notes: Signal plus simple
Plus gde gamme en vecteur de diffusion car SWING : plus d’info notamment les NWs

## Slide 61
Au NWs : self assembly in solution
Expanded hexagonal superlattice
a = 9,7 nm
d = 8,0 nm = 4 * OY length
Au NWs : stabilised by
bilayers of oleylamine !
A. Loubat et al. Langmuir, 2014
Notes: Signal plus simple
Plus gde gamme en vecteur de diffusion car SWING : plus d’info notamment les NWs

## Slide 62
Au NWs : surface stabilisation
N 1s
Cl 2p
Purified Au NWs : XPS and NMR analysis
NH3+
NH2
Au NWs stabilised by bilayers :
Oleylamine (NH2)
Oleylammonium chloride (NH3+, Cl-)

## Slide 63
Au NWs : “zip mechnanism” in micelles
Theoretical simulations
Romuald
Poteau
Oleylammonium chloride (NH3+, Cl-)
at the surface : charges backbone?
A. Loubat et al. J. Phys. Chem. C 119, 4422 (2015)
Gao, J.; Bender, C. M.; Murphy, C. J. Langmuir 19, 9065 (2003)